Fiber optic innovator

Filter WDM (980/1064, 980/1550, 1064/1030, 1550/1064 1480/1550nm)

| Features |  |
| --- | --- |
| Low Insertion Loss & High Isolation High Stability and reliability |  |
| Application |  |
| Fiber Amplifier Fiber Laser Fiber Instrument |  |

Specifications

| Type Parameter | 1480/1550 | 980/1064 | 980/1550 | 1064/1030 | 1550/1064 |
| --- | --- | --- | --- | --- | --- |
| Pass wavelength (nm) | 1530-1580 (or 1440-1490) | 960-990 (or 1020-1080) | 1520-1600 | 1064+/-2.5 | 1500~1600 |
| Reflection wavelength (nm) | 1440-1490 (or 1530-1580) | 1020-1080 (or 960-990) | 965-1000 | 1030+/-10 | 1040~1064 |
| Pass insertion loss (dB) | ≤0.6 | ≤0.8 | ≤0.8 | ≤0.8 | ≤0.8 |
| Reflection insertion loss (dB) | ≤0.5 | ≤0.6 | ≤0.6 | ≤0.6 | ≤0.6 |
| Pass channel isolation (dB) | ≥30 | ≥25 | ≥30 | ≥25 | ≥25 |
| Reflection isolation (dB) | ≥13 | ≥13 | ≥18 | ≥13 | ≥13 |
| Channel flatness (dB) | ≤0.3 | ≤0.3 | ≤0.3 | ≤0.3 | ≤0.3 |
| Directivity (dB) | ≥55 |
| Return loss (dB) | ≥50 |
| PDL (dB) | ≤0.1 |
| Wavelength thermal stability (nm/℃) | ≤0.003 |
| Insertion loss thermal stability( | ≤0.005 |
| Power handling (mW) | ≤300 |
| Operating temperature (℃) | 0 ~ +70 |
| Storage temperature (℃) | -40 ~ +85 |
| Dimensions (mm) | φ5.5×L34 |

Package Dimensions

Ordering Information

| FWDM | Wavelength | Pigtail Type | Fiber Type | Length | Connector |
| --- | --- | --- | --- | --- | --- |
|  | 1064T/1030R 980T/1064R 980R/1064T 1550T/980R 1480T/1550R 1550T/1480R 1550T/1064R | 250=250um bare fiber 900=900um loose tube 3000=3mm loose tube | 1=SMF-28e 4=HI1060 | 1= 1m | NE=None FA=FC/APC FC=FC/UPC SA=SC/APC SC=SC/UPC LC=LC/UPC XX=Other |

www.htopto.com